## Slide 1: February 10 Update
Like in january but a month later

## Slide 2: Testing Data, Young’s Modulus
Note: Only 1 T4 repaired sample. But looks consistent

## Slide 3: T1 Max Load

## Slide 4: T4 Max Load

## Slide 5: Testing Data

## Slide 6: Testing Data
Stress data very consistent across parts at each infill
Strain data not consistent
  Breaks before Ultimate Stress
  Does not have a pattern for when it breaks

## Slide 7: Testing Data
80% infill stronger than 100% infill
Notes: “In the case of 80% infill density, result shows ductile behaviour. This may be due to the fact that there is a minor air gap between the beads and during tensile loading some beads filled this gap. Thus it gave more elongation as compared to specimen built with 100% infill density.”
https://journals.sagepub.com/doi/full/10.1177/0954406219856383

## Slide 8: Semester Timeline