## Slide 1: Updates
05/05/2021

## Slide 2: Gantt
https://docs.google.com/spreadsheets/d/1oa-Z-vQIIZ6xVn4PNoHb93SB0EdPG6uHLpalY9HMLck/edit#gid=0

## Slide 3: Experimentation Variables
Damage Geometry
  T1, T4
Compression vs tension
Infill percentage
  20%,40%,60%,80%,100%
Infill pattern
  Rectilinear (All initial tests done in rectilinear)
  Hexagonal
  Concentric(aligned)
Material
  Pla
  ABS
  Carbon Fiber PLA

## Slide 4: Printing patterns

## Slide 5: Printing done
6 samples each of T1 40,60,80 % rectilinear for compression
All T1 aligned (concentric) finished
  40,60,80% for tension and compression
Summer Work: ABS and Carbon Fiber printing

## Slide 6: Printing base structures (damages)
T1
T4

## Slide 7: Experimentation
New Data
  Working through aligned pieces
  T1 40% aligned tension
  T1 40% aligned compression
  T1 80% hexagonal compression
  T1 60% hexagonal compression
  Aidan's Bars
    Need Eric’s data to compare
40% infill has most patterns finished
  Compression is the strongest
  Hexagonal is very close to rectilinear in tension
  Aligned is greater than both in tension

## Slide 8: Summary/Findings
Compression always stronger than tension
  In some cases stronger than the control
T1 and T4 repairs in tension are similar
  T1 stronger in compression
Strength generally increase with percentage infill
  80% infill stronger than 100%
Initial results from Infill Pattern testing
  Hexagonal and Rectilinear have similar strength in tension
  Aligned is stronger than both in tension
  Aligned is stronger than hexagonal in compression